| 样 品 承 认 书 |
| --- |
| 客户 ： 客户编号 ： |
| 供 应 商 ：嘉兴佳利电子有限公司 产品型号 ：DA51575R18C14 产品描述 ：18*18*4.0mm/NITTO 5000NS/PIN1.5mm 备注 ： |
| 客户签名 : 客户盖章: 公司签名: 公司盖章: 注: 确认后请回传该页！ |
| 制作： | 日期： | 地址 | 浙江省嘉兴市塘汇经济开发区正原路66号 |
|  |  | 电话 | 0573-83651818 |
|  |  | 传真 | 0573-83651858 |

| 版本 日期 版本描述 拟制 审核 批准 V1.0 2018/08/30 首次发行 郁志强 高生 葛伟平 |
| --- |
| 拟制Prepared by： | 审核Checked by ： | 批准Approved by： | 中国浙江省嘉兴市经济开发区塘汇工业区正原路66号 No.66 ZhengyuanRoad, Tanghui Industrial Zone, Jiaxing,Zhejiang,China |
| Formed On： | DOCUMENT Name | DA51575R18C14 | PAGE REV. |
|  |  |  | P2 |

| 目录： 1、 概述 INTRODUCTION 2、 型号 Part Number 3、 结构及材料 Structure and Material 4、 外形尺寸 Dimension 5、 电气性能 Electrical Characteristics 6、 特性曲线 Characteristic curve 7、 包装 Package 8、 环境试验 Environmental specifications 9、 注意事项 Note |
| --- |
| 拟制Prepared by： | 审核Checked by ： | 批准Approved by： | 中国浙江省嘉兴市经济开发区塘汇工业区正原路66号 No.66 ZhengyuanRoad, Tanghui Industrial Zone, Jiaxing,Zhejiang,China |
| Formed On： | DOCUMENT Name | DA51575R18C14 | PAGE REV. |
|  |  |  | P3 |

| 概述 INTRODUCTION "佳利"微波介质天线系列产品用于GPS和局域网产品中，采用右旋圆极化设计，扁平状小型结构，具有低反射损耗、轴比小、增益高的特点。 "GLEAD" microwave dielectric antenna elements and its series are designed to be used for GPS and WLAN. The patch antenna with compact size incorporates a rectangular micro-strip design for GPS C/A right-hand circular polarization wave reception, featuring low RL, low Axial Ratio but high gain, etc. 2. 型号 Part Number DA S 1575 R 18 C1 4（test ground） 厚度 thickness：4mm 中心频率 Center frequency：1576Mhz 外形尺寸：18mm×18mm 极化方式：R=右旋圆极化 polarization：R=Right-hand circular 特征频率Character Frequency：1575 MHz 结构Structure: 单偏 Single Deviation 正方形介质天线 Square Dielectric Antenna |
| --- |
| 拟制Prepared by： | 审核Checked by ： | 批准Approved by： | 中国浙江省嘉兴市经济开发区塘汇工业区正原路66号 No.66 ZhengyuanRoad, Tanghui Industrial Zone, Jiaxing,Zhejiang,China |
| Formed On： | DOCUMENT Name | DA51575R18C14 | PAGE REV. |
|  |  |  | P4 |

| 3. 结构及材料 Structure and Material 表1 No. Description 名称 Structure and Material 结构及材料 4.1 Antenna Substrate 天线基片 Dielectric Ceramics 介质陶瓷 4.2 Pin 引脚 Copper and tinplated 铜镀锡合金 4.3 Electrode 电极 Ag Plated 镀银 4.4 Ground Base 接地面 Ag Plated 镀银 4.5 Adhesive type 双面胶 NITTO 5000NS 4. 外形尺寸 Dimension 图1 dimension |
| --- |
| 拟制Prepared by： | 审核Checked by ： | 批准Approved by： | 中国浙江省嘉兴市经济开发区塘汇工业区正原路66号 No.66 ZhengyuanRoad, Tanghui Industrial Zone, Jiaxing,Zhejiang,China |
| Formed On： | DOCUMENT Name | DA51575R18C14 | PAGE REV. |
|  |  |  | P5 |
| 5. 电气性能 Electrical Characteristics 表2 No. Item (项目) Specifications (特性) Post Environmental Tolerance (环境试验后允许误差) 5.1 接收频率范围 (Mhz) Range of Receiving Frequency GPS：1575.42 ±2.5 5.2 中心频率Center Frequency (Mhz) (with AMT01 GND Plane) 1576 ±2.0 5.3 带宽Band With (Mhz) (Return loss ≤-10dB) ≥5 —— 5.4 驻波比 V.S.W.R(in Center Frequency) ≤1.5 —— 5.5 增益 Gain(Zenith) (dBi typ) | 2 dB typical —— 5.6 轴比 Axial Ratio 5 dB max —— 5.7 偏振方式 Polarization 右旋圆极化 Right-Handed Circular —— 5.8 特性阻抗 Im edance（Ω） 50 —— 5.9 频率温度系数（ppm/℃） Frequency Temperature Coefficient 0±10 —— 6. 特性曲线 Characteristic curve |
| 拟制Prepared by： | 审核Checked by ： | 批准Approved by： | 中国浙江省嘉兴市经济开发区塘汇工业区正原路66号 No.66 ZhengyuanRoad, Tanghui Industrial Zone, Jiaxing,Zhejiang,China |
| Formed On： | DOCUMENT Name | DA51575R18C14 | PAGE REV. |
|  |  |  | P6 |

| 7. 包装 Package 包装名称 Package Name 包装数量 Quantity 吸塑盒 Tray ( 50 )pcs/tray 内装盒 Inner Box ( 500 )pcs/box 外包装箱 Outer Box ( 1000 )pcs/box |
| --- |
| 拟制Prepared by： | 审核Checked by ： | 批准Approved by： | 中国浙江省嘉兴市经济开发区塘汇工业区正原路66号 No.66 ZhengyuanRoad, Tanghui Industrial Zone, Jiaxing,Zhejiang,China |
| Formed On： | DOCUMENT Name | DA51575R18C14 | PAGE REV. |
|  |  |  | P7 |

| 拟制Prepared by： | 审核Checked by ： | 批准Approved by： | 中国浙江省嘉兴市经济开发区塘汇工业区正原路66号 No.66 ZhengyuanRoad, Tanghui Industrial Zone, Jiaxing,Zhejiang,China |
| --- | --- | --- | --- |
| Formed On： | DOCUMENT Name | DA51575R18C14 | PAGE REV. |
|  |  |  | P8 |
| 8.环境试验 Environmental specifications 经环境试验后允许比起始读数偏差见表2 Post Environmental Tolerance ( Refer to the table 2 ) 基准条件：温度范围 Temperature range 25±3℃ 相对湿度范围 Relative Humidity range 55~75%RH 工作温度 Operating Temperature range -40℃~+85℃ 贮藏温度 Storage Temperature range -40℃~+110℃ 8.1 耐湿热特性 Moisture Proof 在温度为40±2℃，相对湿度90~95%的恒温湿箱中放置96小时，在常温中恢复1~2小时后测试，符合表5.1~5.6规定。 The device should satisfy the electrical characteristics specified in paragraph 5.1~5.6 after exposed to the temperature 40±2℃and the relative humidity 90~95% RH for 96 hours and 1~2 hours recovery time under normal condition. 8.2 耐振动 Vibration Resist 将产品刚性固定在试验基板上,在振动频率为10~55Hz振幅为1.5mm 沿X.Y.Z方向各振动2小时后测试符合表5.1~5.6规定。 Take the product is rigidly fixed on the test substrate ,the device should satisfy the electrical characteristics specified in paragraph 5.1~5.6 after applied to the vibration of 10 to 55Hz with amplitude of 1.5mm for 2 hours each in X , Y and Z directions. |
| 拟制Prepared by： | 审核Checked by ： | 批准Approved by： | 中国浙江省嘉兴市经济开发区塘汇工业区正原路66号 No.66 ZhengyuanRoad, Tanghui Industrial Zone, Jiaxing,Zhejiang,China |
| Formed On： | DOCUMENT Name | DA51575R18C14 | PAGE REV. |
|  |  |  | P9 |
| 8.3 高温特性 High Temperature Endurance 在温度为85±2℃的恒温箱中放置96±2小时，在常温中恢复1~2小时后测试。符合表5.1~5.6规定。 The device should satisfy the electrical characteristics specified in paragraph 5.1~5.6 after exposed to temperature 85±2℃for 96±2 hours and 1~2 hours recovery time under normal temperature. 8.4 低温特性 Low Temperature Endurance 在温度为-40℃±2℃低温箱中放置96±2小时后恢复1~2小时测试符合表5.1~5.6规定。 The device should also satisfy the electrical characteristics specified in paragraph 5.1~5.6 after exposed to the temperature -40℃±2℃for 96±2 hours and to 2 hours recovery time under normal temperature. 8.5 焊锡结合力 Adhesion Strength of Soldering 用2Kg力在馈针轴向用力10S，保证外观不损伤，满足5.1~5.6规定。 Force of 2kg is applied to each lead in axial direction for 10s±1 s (see drawing). No visible damage and the device should also satisfy the electrical characteristics specified in paragraph 5.1~5.6. 9.注意事项Note 本承认书保证我司产品作为一个单体时的质量情况。当我司产品被安装到贵司产品上时，请保证贵司的产品已根据贵司的规范进行了有效评价和确认.This product specification guarantees the quality of our product as a single unit. Please make sure that your product is evaluated and confirmed against your specifications when our product is mounted to your product. 2．如果贵司对我司产品的使用已超过了本测试规范所界定的产品功能，那么对于由此引发的失效，我司将不予保证。 We cannot warrant against failure caused by any use of our product that deviates from the intended use as described in this product specification. 3．对于正常使用过程中造成的失效，在出厂之日起三个月内给予免费维修；超过这个时限的维修我们将收取一定的材料成本和维修费用。 The product will get free warranty for three months since the date of purchase users operate in the correct way; users will have to pay cost of the materials and maintaining fee out of the condition. 4．电子敏感元器件，拿起时注意防静电。Electrostatic sensitive device. Observe precautions for handling. 5.产品易受潮，拆封后需24小时内用完，否则剩余部分需真空密封保存。 This item is easy to be moisture. It should be used up within 24h after opening. Otherwise, the rest part needs to vacuum sealed. . |
| 拟制Prepared by： | 审核Checked by ： | 批准Approved by： | 中国浙江省嘉兴市经济开发区塘汇工业区正原路66号 No.66 ZhengyuanRoad, Tanghui Industrial Zone, Jiaxing,Zhejiang,China |
| Formed On： | DOCUMENT Name | DA51575R18C14 | PAGE REV. |
|  |  |  | P10 |